## Slide 1: Introduction to PAOFLOW Marco Buongiorno Nardelli University of North Texas and Santa Fe Institute

## Slide 2: Some QE post processing

## Slide 3: QE post processing

## Slide 4: QE post processing

## Slide 5: QE post processing

## Slide 6: QE post processing

## Slide 7: QE post processing

## Slide 8: Localized orbitals

## Slide 9: Localized basis sets
Chemical interpretation of the wavefunction
Simple connection with plane-waves via Fourier transforms:
  Construction of model Hamiltonians (e.g. strongly correlated systems)
  Band structure interpolation
  Transport properties
  Many more…
Bloch states (plane waves)
Localized states (i.e. atomic orbitals)

## Slide 10: Wannier functions
A convenient localized basis set.
Maximal localization: Unique basis set
Not straightforward (what projectors and how many?)
Internal iterative procedure for disentangling bands (e.g in metals)
  Energy window?
  Intractable for large number of bands
Bloch
Wannier
N. Marzari et. al. Rev. Mod. Phys. 84, 1419 (2012)

## Slide 11: Localized basis sets
Chemical interpretation of the wavefunction
Simple connection with plane-waves via Fourier transforms:
  Construction of model Hamiltonians (e.g. strongly correlated systems)
  Band structure interpolation
  Transport properties
  Many more…
Bloch states (plane waves)
Localized states (i.e. atomic orbitals)

## Slide 12: The PAOFLOW method

## Slide 13: Pseudo-atomic orbitals (PAO)
Readily available from pseudo-potentials:
Connection to Bloch states (i.e Kohn-Sham states from DFT) via a simple projection -- typically done to obtain Projected Density of States (PDOS):
We assume the basis is orthonormal
Silicon

## Slide 14: QE post processing
proj.in
< proj.in

## Slide 15: Hands-on: Silicon – PDOS
pw.x < scf_Si.in > scf_Si.out
projwfc.x < proj.in > proj.out
sumpdos *\(x\)* > X.dat (for the x orbitals) or sumpdos silicon.pdos_atm#X1\(* > atomX.dat (for the X atom)

## Slide 16: Hands-on: Silicon – PDOS
Atomic states used for projection
(read from pseudopotential files):
state # 1: atom 1 (Si ), wfc 1 (l=0 m= 1)
state # 2: atom 1 (Si ), wfc 2 (l=1 m= 1)
state # 3: atom 1 (Si ), wfc 2 (l=1 m= 2)
state # 4: atom 1 (Si ), wfc 2 (l=1 m= 3)
state # 5: atom 1 (Si ), wfc 3 (l=2 m= 1)
state # 6: atom 1 (Si ), wfc 3 (l=2 m= 2)
state # 7: atom 1 (Si ), wfc 3 (l=2 m= 3)
state # 8: atom 1 (Si ), wfc 3 (l=2 m= 4)
state # 9: atom 1 (Si ), wfc 3 (l=2 m= 5)
state # 10: atom 1 (Si ), wfc 4 (l=3 m= 1)
state # 11: atom 1 (Si ), wfc 4 (l=3 m= 2)
state # 12: atom 1 (Si ), wfc 4 (l=3 m= 3)
state # 13: atom 1 (Si ), wfc 4 (l=3 m= 4)
state # 14: atom 1 (Si ), wfc 4 (l=3 m= 5)
state # 15: atom 1 (Si ), wfc 4 (l=3 m= 6)
state # 16: atom 1 (Si ), wfc 4 (l=3 m= 7)
state # 17: atom 2 (Si ), wfc 1 (l=0 m= 1)
state # 18: atom 2 (Si ), wfc 2 (l=1 m= 1)
state # 19: atom 2 (Si ), wfc 2 (l=1 m= 2)
state # 20: atom 2 (Si ), wfc 2 (l=1 m= 3)
state # 21: atom 2 (Si ), wfc 3 (l=2 m= 1)
state # 22: atom 2 (Si ), wfc 3 (l=2 m= 2)
state # 23: atom 2 (Si ), wfc 3 (l=2 m= 3)
state # 24: atom 2 (Si ), wfc 3 (l=2 m= 4)
state # 25: atom 2 (Si ), wfc 3 (l=2 m= 5)
state # 26: atom 2 (Si ), wfc 4 (l=3 m= 1)
state # 27: atom 2 (Si ), wfc 4 (l=3 m= 2)
state # 28: atom 2 (Si ), wfc 4 (l=3 m= 3)
state # 29: atom 2 (Si ), wfc 4 (l=3 m= 4)
state # 30: atom 2 (Si ), wfc 4 (l=3 m= 5)
state # 31: atom 2 (Si ), wfc 4 (l=3 m= 6)
state # 32: atom 2 (Si ), wfc 4 (l=3 m= 7)
Our basis or localized orbitals

## Slide 17: Hands-on: Silicon – PDOS
Lowdin Charges:
Atom # 1: total charge = 3.9897, s = 0.9061,
Atom # 1: total charge = 3.9897, p = 2.3837, pz= 0.7946, px= 0.7946, py= 0.7946,
Atom # 1: total charge = 3.9897, d = 0.6981, dz2= 0.0861, dxz= 0.1753, dyz= 0.1753, dx2-y2= 0.0861, dxy= 0.1753,
Atom # 1: total charge = 3.9897, f = 0.0018, fz3= 0.0003, fxz2= 0.0002, fyz2= 0.0002, fzx2-zy2= 0.0002, fxyz= 0.0003, fx3-3xy2= 0.0003, f3yx2-y3= 0.0003,
Atom # 2: total charge = 3.9897, s = 0.9061,
Atom # 2: total charge = 3.9897, p = 2.3837, pz= 0.7946, px= 0.7946, py= 0.7946,
Atom # 2: total charge = 3.9897, d = 0.6981, dz2= 0.0861, dxz= 0.1753, dyz= 0.1753, dx2-y2= 0.0861, dxy= 0.1753,
Atom # 2: total charge = 3.9897, f = 0.0018, fz3= 0.0003, fxz2= 0.0002, fyz2= 0.0002, fzx2-zy2= 0.0002, fxyz= 0.0003, fx3-3xy2= 0.0003, f3yx2-y3= 0.0003,
Spilling Parameter: 0.0026

## Slide 18: Pseudo-atomic orbitals (PAO)
Readily available from pseudo-potentials:
KS eigenvalues
LCAO
Hamiltonian
Si (2s22p2 basis set): 8 atomic orbitals
Valence bands reproduced to high accuracy
Conduction bands deviate strongly from KS eigenvalues.
L. A. Agapito et. al. Phys. Rev. B 88, 165127 (2013)
Connection to Bloch states (i.e Kohn-Sham states from DFT) via a simple projection -- typically done to obtain Projected Density of States (PDOS):

## Slide 19: Projectability of bands
LCAO band structure with spd basis set.
  Some low energy conduction bands improve.
  A set of null eigenvalues are inserted
Projectability:
High projectability bands (i.e. Pn ≈ 1) yield accurate LCAO band structure.
Low projectability bands (i.e. Pn << 1) yield poor LCAO bands and lead to null eigenstates.

## Slide 20: Accurate PAO Hamiltonians
bands
plane
waves
atomic
orbitals
GOOD
projectability
BAD
projectability
20

## Slide 21
21
Exclude the bad projectability states from the set of bands to be represented (filtering) – orthogonal projection
Introduces a spurious null space that must be eliminated
Shift by a fixed energy outside of the region of good projectability bands
(shifting)

## Slide 22: Accurate PAO Hamiltonians
22

## Slide 23: Accurate PAO Hamiltonians
Effective description of entangled bands in metals
Mo
Cu
projections
Wannier functions

## Slide 24: PAOFLOW
Go to the Example1 directory on the tutorial repository
Run scf.in and nscf.in
Go to the jupyter notebook!

## Slide 26
Construction of PAO Hamiltonians from the DFT wavefunctions onto pseudo atomic orbitals
Construction of PAO Hamiltonians from analytical tight binding models
Hamiltonian data for further processing (ACBN0, PAOtransport, etc.)
External fields and non scf ACBN0 correction
Spin orbit correction of non SO calculations
Bands along standard paths in the BZ
Real space electronic charge density
Interpolation of Hamiltonians on arbitrary Monkhorst and Pack k-meshes
Adaptive smearing for BZ and Fermi surface integration
Density of states (and projected DOS)
Fermi surfaces and spin textures
Boltzmann transport (conductivity, Seebeck coefficient, electronic contribution to thermal conductivity
dielectric function (absorption coefficients and EELS)
Berry curvature and anomalous Hall conductivity (including magnetic circular dichroism spectra)
spin Berry curvature and spin Hall conductivity (including spin circular dichroism spectra)
Band topology (Z2 invariants, Berry and spin Berry curvature along standard paths in BZ, critical points
PAOFLOW capabilities

## Slide 27: K-point interpolation
27
Convergence of multi-valley bands as the electronic origin of high thermoelectric performance in CoSb3 skutterudites, Y. Tang, Z.M. Gibbs, L.A. Agapito, G. Li, H. Kim, M. Buongiorno Nardelli, S. Curtarolo and G.J. Snyder

## Slide 28: Transport properties
The standard approaches to electron transport in bulk semiconductors are based on the semiclassical Boltzmann theory.
Dynamics of carriers and response to external fields follow classical motion equation, whereas scattering events are included in a perturbative approach, via quantum mechanical Fermi Golden Rule.

## Slide 29: Semiclassical transport
probability density distribution function:
equation of motion:
relaxation-time approximation:
Fermi Golden Rule:
Boltzman conductivity:

## Slide 30: Boltzmann Transport Equations
Accurate evaluation of Boltzmann transport integrals:
Band velocities:
Scattering time:
Fermi-Dirac distribution:
Requires very fine sampling of bands around Fermi energy – projection Hamiltonian!
e.g. Seebeck coefficient of Bi2Te3

## Slide 31: Increase the basis set

## Slide 32: PAOFLOW internal bases (go to jupyter notebook)

## Slide 33: Some more advanced applications (go to jupyter notebook)

## Slide 34: Berry curvature and Anomalous Hall conductivity: Fe
Berry curvature from Kubo formula:
Anomalous Hall conductivity:

## Slide 35: Spin Hall conductivity

## Slide 36
MoTe2: A Type-II Weyl Topological Metal
Wang et al., 10.1103/PhysRevLett.117.056805
z2pack.ethz.ch/doc/2.1/index.html
Topological invariants

## Slide 37
Nodal chain and Weyl points in HfC

## Slide 38
example01 : Si with spd pseudpotential
example02 : Al with spd pseudpotential
example03 : Pt with lsda (nspin = 2)
example04 : Fe non collinear with spin orbit - Anomalous Hall conductivity
example05 : Pt non collinear with spin orbit - Spin Hall conductivity
example06 : AlP with non self consistent ACBN0
example07 : Al starting from projections with overlap matrix of the atomic orbital (prior to orthogonalization)
example08 : 2D SnTe - Spin Hall conductivity
example09 : Weyl point search in MoP2
example10 : Transport in GaAs with temperature and energy dependent model for relaxation time
PAOFLOW Examples